## Slide 1: Concrete Analysis
Predicting Failure in Fibre-Reinforced Concrete
Insert Names Here PLS

## Slide 2: The Data
Sourced from a series of experimental trials by the SIKA
Contains 1440 observations and 10 variables, 7 of which are used as independent variables while the remaining 3 are dependent

## Slide 3: The Data
Sourced from a series of experimental trials by the SIKA
Contains 1440 observations and 10 variables, 7 of which are used as independent variables while the remaining 3 are dependent

## Slide 4: The Goal – 2 Level Predictive Modeling
1. Level Hypothesis: IFSS
Interfacial sheer strength (IFSS) can be sufficiently predicted through the profile area, fibre length, avg. fibre circumference and Titer.
2. Level Hypothesis: Minibeam energy absorption
IFSS and fibre tenacity can be used to sufficiently predict Minibeam energy absorption and subsequently failure.

## Slide 5: The Goal – Flowchart 2 Level Predictive Modeling
1. Level
W_Sm
W_q
Profile Area
Fibre length
Titer
Avg. circumference
predict
calculate
IFSS
Fibre Tenacity
predict
Minibeam energy absorption
calculate
Failure mode
2. Level

## Slide 6: The Catch
In the Field, it is common that not all parameters are known
To be applicable to the real-world, this issue has to be dealt with
Prediction of missing parameters is often not possible
Solution:
Create multiple models and figure out which works best for which missing data
Incorporate a decision-tree approach were the most reliable model is chosen for the situation

## Slide 7: The EDA
No significant outliers found with z-scores > 3 or <-3
Some significant correlations found through PearsonsR
Some unexpected correlations with fibre length
Not a perfect correlation between failure mode and energy absorption

## Slide 8: The EDA
No significant outliers found with z-scores > 3 or <-3
Some significant correlations found through PearsonsR
Some unexpected correlations with fibre length
Not a perfect correlation between failure mode and energy absorption

## Slide 9: The PCA
Suggests dimensionality reduction to 4 or 5 principal components
Due to the relatively small size of the data and the ease of computing, we chose to continue to utilize the full dataset w/o Profile Area to increase prediction quality

## Slide 10: The Models
Suggests dimensionality reduction to 4 or 5 principal components
Due to the relatively small size of the data and the ease of computing, we chose to continue to utilize the full dataset w/o Profile Area to increase prediction quality